 
HBI SPECIFICATIONS

	HOT BRIQUTTED IRON

	CHEMICAL PROPERTIES

	Total Iron
	90.0% Min

	Metallic Iron
	84.0 %Min

	Metallization
	93.0 % Min

	Carbon
	1.3 - 1.6 %

	Total Gangue             (SiO2+Al2O3+CaO+MgO)
	6.0% max

	Sulphur
	0.005% Max

	Phosphorus
	0.06% Max

	PHYSICAL PROPERTIES

	Bulk Density
	2.4-2.7 Tons/M3

	Apparent Density
	4.7-4.9 gm/cc 

	Under size <6.3 mm
	5% Max


